Teraco lité  s.r.o.

Toužimská 588/70,  197 00 Praha

IČO: 24230456	                   Tel: 605316727

DIČ: CZ24230456

Zapsána u  Městského Soudu  v Praze, C/200327

KB Dvůr Králové n.l., 	                    E-mail:

Číslo účtu: 107-3990700287/0100   teracolite@atlas.cz

www.terrazzodecor.cz

Subject: Technological procedure

## Action:

Cast terrazzo floors from polymer-cement matrix.

Building preparedness

The substrate for cast terrazzo must be at least B 20 or higher. The thickness of the concrete should be at least 60 mm. Before laying terrazzo, the concrete foundation should be at least 14 days old and shrunken, so that possible cracks could be repaired. For floors, it must be reinforced with steel reinforcement – a reinforcement mesh of at least 100x100x6 mm. The meshes are always laid as a whole without interruption. In the case that concrete with dispersed reinforcement is used, it depends on the concrete supplier´s recommendations. Dilations are subsequently cut, any dilations in the substrate are always accorded in the given place, otherwise there is a risk of rupture of the terrazzo outside the expansion joint strip. Dilations may drift from the direction by max. 7 mm on each side. Terrazzo is a supporting component and always copies the properties of the substrate. Concrete must always be laid continuously, without working or technological gaps. All such joints must be allocated by dilation. This is very important, since the expansion joint strip is the ultimate facing element. Recommended expansion units are 4500x4500 mm. The concrete surface must be smooth, without cement residues. The substrate is laid to a level minus 15-20 mm below net height. Possible floor heating, if any, must already be incorporated into the concrete substrate, it cannot be embedded into the terrazzo matter. All installations and wiring must be below any fixtures.

Terracco laying:

The base must be properly cleaned and deprived of any deposits of building materials. The substrate is completely penetrated using a primer. In the case that the thickness of terrazzo layers exceeds the thickness by more than 20 mm, the level of the substrate must be adjusted. The leveling of the substrate is not a standard part of the terrazzo and material with very high adhesion must be used. After preparing the substrate, expansion joint strips, which at the same time also serve as a guide strips for levelling the terrazzo matter, are placed. Terrazzo is mixed with fractions and colour shades of crunched material determined by the architect or investor. The ratio of water and terrazzo is determined by the supplier, depending on weather conditions. After laying the terracco, the surface becomes hard enough to walk on after about 2 hours, fully supporting after 7 days.

See Technical data sheet.

Terracco grinding:

Cement-based Terrazzo from polymer-cements can be ground after 24 hours. Terrazzo is ground either under water, which is standard for large areas, or dry. Terrazzo is ground in a few steps from 00 up to the finest 800. At the grinding stage with 220, the entire terrazzo area is sealed so as to fill the pores that occur when mixing the mixture. At his point there is also a technological break allowing the sealing compound to harden.

The terrazzo worker determines the break, depending on the weather conditions.

After the bonding agents have hardened, the floor is ground with a fine grinder.

Final surface treatment:

After the final fine grinding, it is necessary to close the terrazzo with wax so that it becomes completely water-repellent. This protects the material against the penetration of dirt and liquids. In the case that the final grinding is carried out under water, it is essential to restrict construction to avoid soiling during drying.

To apply the wax, it is necessary to prevent terrazzo from becoming humid or wet. Terrazzo cannot be covered, since that would prevent it from drying. After the application of the wax, the terrazzo floor is completed and subsequent maintenance is carried out according to the instructions for use.

In Prague dated 01.09.2013